Figure 1: Box plots with whiskers showing the mean and the standard errors of different minerals at different localities.

Figure 2: Plot of means for the different minerals at the cervical, medium, apical and summation sites.

Figure 3: Correlation array for the concentration of different minerals in different study regions.

Figure 4: Scanning electron micrograph of group I (Control) at the cervical third of the root showing a smooth homogenous cementum surface covered by periodontal fibers. ( 1015 x).

Figure 5:  Progressive periodontitis at the cervical third of the root showing irregular rough surface with the presence of multiple deep crack lines (1078 x).

Figure 6: Middle third of the root of progressive periodontitis showing severe destruction of cementum surface with the exposure of the underlying dentin with the presence of multiple craters and deep multiple resorption area (2118x).

Figure 7: Middle third of the root showing severe destruction of cementum surface with the exposure of the underlying dentin with the presence of multiple craters (10865x).

Figure 8: Apical third of the root of progressive periodontitis showing multiple deep defect areas and complete absence of the periodontal fibers (1000 x).