**Abstract**

**Aims:** This study evaluated the bond strength of fiberglass posts (PFV) to radicular dentin in cervical, middle and apical thirds, after using ultrasonically activated irrigants.

**Methods:** One hundred and twenty lower premolars were sectioned, which were distributed into 10 groups (n=12), according to irrigant and ultrasonic treatments. The groups were 2.5% sodium hypochlorite (HS), 2% chlorhexidine digluconate (CL), 17% EDTA, saline (SF) distilled water (AD), plus or minus ultrasonic instrumentation, and posts were cemented whith RelyX ARC.

**Results:** The bond strength was evaluated by means of the push-out test, and results were subjected to repeated measures three-way analysis of variance and Tukey test revealed that compared to EDTA 17%, CL and SF significantly reduced the bond strength of PFV, regardless of ultrasonic instrumentation and also independently from root third (p = 0.015). The most prevalent failure type was adhesive between the dentin and cement for the EDTA and HS groups, followed by mixed failure for the CL and HS groups. PFV bond strength was not affected by ultrasonic instrumentation (p = 0.114), nor was it different between root thirds (p = 0.280).

**Conclusions:** The PFV bond strength to root dentin was influenced by the irrigant used, where the greatest results were obtained with 17% EDTA when compared to CL and SF with or without passive ultrasonic instrumentation.

**Keywords:**

Ultrasonic. Root canal irrigants. Root canal posts. Sodium hypochlorite. Chlorhexidine.

**1. Introduction**

Endodontic treatment is related to the loss of dental structure owing to the presence of caries lesions, old restorations, fractures or access for endodontic preparation. In this context, in order to provide retention for the restoration in this dental element, the use of glass-fiber posts is recommended, which, as they have a high resistance to flexion and modulus of elasticity similar to that of dentin, has made it possible to achieve success rates of between 90% and 99% [1].

Nonetheless, in order to achieve success with rehabilitation procedures, it is also essential that, for endodontic treatment, the remains of the vital and necrotic pulp tissue have been removed, as well as microorganisms and microbial toxins from the root canal system [2]. In this context, it is of paramount importance that irrigants are used which act as cleaning agents during the biomechanical treatment, with the removal of microorganisms, of products associated with tissue degeneration and organic and inorganic residue, ensuring the elimination of the contaminated dentin and permeability along the entire length of the canal [3]).

At this time, there are no irrigants available that combine all of the ideal characteristics, even when used with a lower pH, have a higher temperature or are added to surfactants [4]. There is no single irrigant that has shown itself capable of dissolving organic pulp material and demineralizing the wall of the root canal [5].

Among the auxiliary chemical substances used in endodontics during the chemical/mechanical preparation of the root canals, sodium hypochlorite (NaOCl), in a variety of concentrations (0,5% to 6%), is the one most frequently used [6]. Despite its wide spectrum of antimicrobial action and the property of dissolving organic tissue, its penetration into the dentin tubules is limited [7]. However, it should be stressed that in high concentrations NaOCl has cytotoxic effects, while in low concentrations it is ineffective against *enterococcus faecalis* [8].

The complete cleaning of the root canal system requires the use of irrigants that dissolve both organic and inorganic material. As NaOCl is only active on organic material, another substance may be used to supplement the removal of the smear layer [9]. EDTA has been used for this purpose but, on the other hand, it has little or no effect on organic tissue and has no antibacterial activity [5]. As a chelating agent, EDTA can accelerate the effect of the NaOCl and help to diffuse the hydroxyl ions through the dentin tubules [10]. However, EDTA alters the physical and chemical properties of dentin and increases the adherence of *enterococcus faecalis*, a significant bacteria linked to post-endodontic treatment infections [11,12,8].

Chlorhexidine digluconate at 2% (CHX) has also been suggested as an irrigant for endodontic treatment [13], due to its antimicrobial properties and substantivity [14]. The chlorhexidine gel is an auxiliary chemical substance that does not interfere with the collagen present in the organic matrix of root dentin or the quality of the filling and restoration [15].

Throughout the history of endodontics, efforts have focused on developing more effective systems for applying and agitating irrigant solutions in the canal system [3]. These systems can be divided into two categories of agitation techniques: manual and mechanical [16]. The latter includes the use of simultaneous irrigation with rotating canal instrumentation, pressure switching devices as well as sonic and ultrasonic systems [14]. All of these appear to improve canal cleaning when compared to irrigation with a conventional syringe and needle [14].

The use of ultrasound for irrigation procedures results in a more efficient cleaning of the canals, improves the dissociation of the irrigant in the canal system, provides a softening of the dentin debris and removes bacteria and smear layer. In view of the conflicting, barely explored outcomes, there is a need to conduct fresh studies to investigate the effectiveness of the ultrasound apparatus and its impact on the outcome of treatment [17). This is even more important if we consider the associated presence of the irrigant.

Bearing in mind the above aspects, this study aims to contribute to the understanding of the influence of endodontic irrigating solutions, with and without ultrasonic instrumentation, on the bond strength of fiber posts cemented with resinous agent to the root dentin of human teeth. The null hypothesis tested was that the use of irrigants, both with and without passive ultrasonic instrumentation, does not affect (i) the strength of the bond between glass-fiber posts and radicular dentin, (ii) in either the cervical, middle or apical regions.

**2. Materials and Methods**

2.1 Experimental design

This study followed a randomized complete-block design, with repeated measures, in a 5x2x3 factorial scheme, the factors studied being as follows:

2.1.1 irrigation solution, at five levels (distilled water, saline solution, 2% chlorhexidine digluconate solution, 2.5% sodium hypochlorite and EDTA 17%);

2.1.2 ultrasound, on two levels (present and absent);

2.1.3 root third, on three levels (cervical, mid and apical).

The experimental units consisted of 120 roots of human lower premolars randomly divided into ten groups, according to the irrigation solution and the use, or not, of ultrasound (n = 12). Three cross-sections were obtained from one single experimental unit corresponding to the cervical, middle and apical root thirds, characteristic of a repeated measures experiment. The qualitative response variable was push-out bond strength of the glass-fiber posts cemented to the root canal, measured in MPa. The bond failure mode was a qualitative response variable.

2.1 Ethical aspects

The protocol for this research study was submitted to the Human Research Ethics Committee at the São Leopoldo Mandic Dental Faculty, which approved the use of 120 single-rooted human teeth (lower premolars), donated by the Tooth Bank at the São Leopoldo Mandic Dental Faculty.

2.3 Sectioning of teeth and acquisition of specimens

The premolars were cleaned with scalpel blades, polished using pumice stone and a low-rotation Robinson brush and maintained at 4oC in a solution of 0.1% thymol. The teeth were sectioned at the cementoenamel junction using a low-rotation diamond cutting wheel, under refrigeration (Isomet 2000; Buehler Ltd., Lake Bluff, IL, USA), in order to obtain 120 roots with a length of 16 mm, the measurement of which was performed using a digital micrometer (MIP/E – 103, Mitutoyo Sul Americana Ltda., Suzano, SP, Brazil). The following exclusion criteria were applied: roots with excessive curvature, open root apex and the presence of more than one root canal, appearance being assessed by way of a radiographic examination of the teeth.

2.4 Biomechanical preparation and filling

The root canals were prepared using the step-back technique with K-Files (Dentsply/Maillefer, Petrópolis, Rio de Janeiro, RJ, Brazil). The cervical and middle thirds were enlarged using Gates-Glidden drills (Dentsply/Maillefer, Petrópolis, Rio de Janeiro, RJ, Brazil), prior to canal preparation.

Depending upon the group to which the roots belonged, the canal was irrigated using the following vehicles: distilled water, saline solution, solutions of 2% chlorhexidine digluconate, 2.5% sodium hypochlorite or EDTA (Biodinâmica, Ibiporã, PR, Brazil), both with and without the use of ultrasound (Microssonic, Driller, Carapicuíba, São Paulo, Brazil) using the PUI technique, namely Passive Ultrasonic Irrigation. Ultrasound was used for one minute after instrumentation with the aid of special inserts to cause the irrigant to vibrate. The root canals were irrigated using 20 mL of each solution during the cleaning and instrumentation, and were filled using calcium hydroxide-based cement (Sealer 26, Dentsply, Rio de Janeiro, RJ, Brazil), using the lateral compaction technique.

The bed for the cementation of the posts was prepared at 14 mm using glass-fiber posts (Exacto #1, Angelus, Londrina, PR, Brazil). Special drills were employed supplied by the manufacturer of the system of posts, in order to remove the fillings from the canal, resulting in 2 mm of apical sealing.

2.5 Preparation and cementation of the glass-fiber posts

Prior to cementation, the glass-fiber posts (Exacto #1, Angelus, Londrina, PR, Brazil) were cleaned in 70% alcohol for 1 minute, and then dried. Afterwards, silane agent (Exacto, Angelus, Londrina, PR, Brazil) was applied using disposable microbrushes (Cavibrush 2, FGM, Dentscare, Joinville, SC, Brazil) for 1 minute and then air-dried.

Prior to cementation, the root dentin was etched using 37% phosphoric acid (Condac 37, FGM, Joinville, SC, Brazil) for 15 seconds. After washing, it was dried with absorbent paper (Dentsply/Maillefer, Rio de Janeiro, RJ, Brazil). After testing the post, the adhesive system was applied (Adper Scotchbond Plus, 3M ESPE, St. Paul, MN, USA), with disposable microbrushes (Cavibrush 2, FGM, Dentscare, Joinville, SC, Brasil) and, following the manufacturer’s recommendation, a layer activator was applied (Adper Scotchbond Plus, 3M ESPE, St Paul, MN, EUA) and dried for 5 seconds. Then, a primer layer was aplplied (Adper Scotchbond Plus, 3M ESPE, St Paul, MN, EUA) and dried for 5 seconds. Finally, a catalyst layer (Adper Scotchbond Plus, 3M ESPE, St Paul, MN, USA) was applied to the conduit, being the excesses removed with absorbent paper # 80 (Dentsply/Maillefer, Petrópolis, RJ, Brasil) after each application.

Conventional dual-cure resin cement (RelyX ARC, 3M ESPE, St. Paul, MN, USA) was manipulated following manufacturer’s recommendations, and inserted into the root canal and the post, with the aid of a periodontal probe with millimeter markings. The posts were then placed inside the canal, using finger pressure, for 3 minutes, the excess cement being removed. The light-activation was then carried out through the post in the occluso-apical direction for 40 seconds, with the light-activation unit (GNATUS, Ribeirão Preto, SP, Brazil). The samples were stored iat 100% relative humidity.

2.6 Acquiring the samples

After storage in an environment whit 100% relative humidity of 4ºC, the specimens were fixed to acrylic plates with wax for sculpting (Kota, São Paulo, SP, Brazil) such that the long axis of the post was parallel to the plate surface and perpendicular to one of its edges and then sectioned in a precision cutter (Isomet 1000, Buehler Ltd., Bluff, IL, USA), using a high-concentration diamond cutting wheel (Buehler Ltd., Bluff, IL, USA). Cuts were made in the buccolingual direction of the root, so as to obtain sections 1 mm thick for each of the thirds, cervical, middle and apical.

Once the specimens were obtained, the diameters of the canal on the cervical and apical surfaces were measured and the height was measured using a digital micrometer (MIP/E – 103, Mitutoyo Sul Americana Ltda., Suzano, SP, Brazil).

2.7 Push-out bond strength test

The push-out bond strength test was conducted using a universal testing machine (EZ-LX, Shimadzu Corporation, Suzhou, Jiamgsu, China), at a speed of 0.5 mm/min, attached to a 500 N load cell. The slices were placed in a device such that the force was applied in the apical-cervical direction by means of a metal piston measuring 1 mm in diameter, until the post was dislodged.

The bond strength values, in MPa, were obtained by dividing the force used to provoke the failure (in Newtons) by the glued area (in mm2). To calculate the glued surface area, taking into account the conical shape of the posts, the following formula was applied:

**Area = π (R + r) [h2 + (R - r)2]0.5**, where:

R – radius in the cervical portion (mm)

r – radius in the apical portion (mm)

h – slice thickness (mm)

2.8 Evaluation of failure mode

An analysis of the failure pattern at the dentin-cement-post interfaces was performed using a stereoscopic magnifier (EK3ST, Eikonal Equip. Ópticos e Analíticos, São Paulo, SP, Brazil), at a magnification of 40x. Failure types were classified as:

a) adhesive between cement and dentin;

b) adhesive between cement and post;

c) cohesive: dentin;

d) mixed, with cohesive and adhesive fracture

2.9 Statistical analysis

The bond strength values were evaluated for compliance with the assumptions of normality and homoscedasticity, by means of the Shapiro-Wilk and Levene tests, respectively, applying the square root transformation for variance stabilization.

The transformed data were subjected to a three-way analysis of variance for repeated measures and the Tukey test for multiple comparisons.

The statistical calculations were performed using the software program SPSS 20 (SPSS Inc., Chicago, IL, USA), using a level of significance of 5%.

**3. Results**

Table 1 shows the descriptive analysis, in terms of means and standard deviations, of the push-out bond strength values of glass-fiber posts to the radicular dentin, subjected to irrigation with different agents, whether or not associated with the use of ultrasonic agitation, and by root third.

The three-way analysis of variance showed that there was no significant interaction between the factors being studied, *Irrigation solution, Ultrasound* and *Root third* (p = 0.220). The dual interactions *Irrigant vs. Ultrasound* (p = 0.384), *Irrigant vs. Root third* (p = 0.870) and *Ultrasound vs. Root third* (p = 0.125) were also not significant.

Regardless of whether or not PUI was used and of root third, it was found that bond strength was influenced by the irrigating agent (p = 0.015). The Tukey test identified that, when irrigation was carried out using 2% chlorhexidine digluconate and with saline solution, significantly lower bond strength values were found for the glass-fiber post to the root canal versus the groups in which irrigation was conducted with EDTA at 17%. As for the groups where the irrigating agent was 2.5% sodium hypochlorite and distilled water, it was found that bond strength did not differ significantly from that found in the groups irrigated with EDTA at 17%, chlorhexidine digluconate at 2% and with saline solution (Table 1).

The three way analysis of variance for repeated measures also showed that, for any of the irrigating agents used and location of the root third, the PUI did not have any effect on the bond strength of the glass-fiber post to the radicular dentin (p = 0.114).

Finally, through the three way analysis of variance for repeated measures, no significant difference was found for bond strength values obtained in the cervical, middle and apical thirds (p = 0,280).

Figure 1 shows the fracture modes exhibited by the samples after the push-out bond strength test indicating that the adhesive failure between the dentin and cement was the most prevalent failure mode when using the irrigants EDTA at 17% and 2.5% sodium hypochlorite, regardless of whether or not PUI was performed. This was followed by mixed failure whose highest index occurred when using the irrigants 2% chlorhexidine digluconate and 2.5% sodium hypochlorite. Failures of the post-cement adhesive type and cohesive type in dentin demonstrated the lowest indices, had been performed.regardless no matter whether or not PUI and of the apical third

**4. Discussion**

In the present study, it was found that bond strength was influenced by the irrigation agent, no matter whether or not passive ultrasonic instrumentation was performed, thereby rejecting the null hypothesis. Irrigation with EDTA at 17% provided significantly higher bond strength values than when carried out with 2% chlorhexidine digluconate and saline solution. This result may be explained by the fact that EDTA is effective in removing the smear layer in root canals, providing a dentin surface free from residue and wider open dentinal tubules [18,19,17,20], facilitating the penetration of the resin cement after preparing the space for the cementation of posts in endodontically treated teeth [ 21,22,23,20].

Moreover, it has been reported that EDTA is the best solution for removing the smear layer during the use of both sonic irrigation [24,25,26] and ultrasonic irrigation [27,28,19], provided it is used for no longer than one minute, as over longer periods of time it could result in excessive dentin erosion [29], which justifies the use of ultrasonically activated EDTA, for one minute, in the present study. On the other hand, [19], used EDTA 17% after instrumentation for three minutes, ultrasonically activated and prior to the final irrigation with solutions of 2.5% and 5.25% NaOCl, saline solution and 2% chlorhexidine gel, respectively, obtaining a lower bond strength in the group irrigated with 5.25% NaOCl and the use of the self-adhesive resin cement RelyX U100, which differs from the present study in that there was no statistically significant difference between the groups, either with or without ultrasonic activation, when using dual-cure resin cement RelyX ARC. The difference in outcomes may be associated with the fact that the aforementioned researchers used the cement RelyX U100 which, due to its relatively high viscosity, combined with its low demineralizing capacity, may have contributed to low infiltration of the monomer into the dentin, thereby reducing micromechanical retention [30].

Distilled water and the 2.5% sodium hypochlorite solution were no different from either EDTA at 17% or 2% chlorohexidine digluconate solution and saline solution. 2.5% sodium hypochlorite has a wide spectrum of antimicrobial action and the property of dissolving both organic and inorganic tissue, although it is not effective in removing the smear layer and dentin debris from the root canal walls, which could affect the bond strength of the glass-fiber post [7,9]. Combined with these factors, sodium hypochlorite breaks down into sodium chloride and oxygen [31]. It has been reported that this release of oxygen inhibits the polymerization of resin cements, leading to a reduction in bond strength [20]. In this study, the fact that sodium hypochlorite did not result in lower adhesion values when compared to the other irrigants employed is probably attributable to the concentration applied (2.5%), a finding which corroborates the results of [19], who highlighted that sodium hypochlorite in the aforementioned concentration did not interfere with the bonding capacity of resin materials to the radicular dentin.

In this study, irrigation with chlorhexidine digluconate did not result in an improvement in bond strength, in agreement with the results of earlier studies, probably due to its inability to dissolve organic and inorganic material, making it difficult to clean the root canal walls, in other words, the presence of debris and smear layer create a physical barrier, obstructing the dentinal tubules, preventing the penetration of the adhesive system and reducing the interaction of the resin cement with the dentin surface [32,33,34].

Another factor which must be taken into consideration in this study is that the PUI had no effect on the bond strength of the glass-fiber post to the radicular dentin, regardless of the irrigation agent employed and the location of the root third. One explanation for this finding may lie in the fact that PUI does not significantly improve the removal of smear layer on the dentin [23]. In fact, despite the fact that PUI is better than irrigation with needles, it is reported that the smear layerwas not completely eliminated [22]. It should be stressed, however, that in this study the solution of sodium hypochlorite used had more than double the concentration of that used by the aforementioned authors, being applied for 60 seconds, six times greater, which may explain the fact there was no significant difference between the groups in which ultrasound was or was not used.

In terms of the removal of smear layer, several studies have produced conflicting results, probably due to the different concentrations of irrigation solutions and the length of time activated inside the canal [35]. As far as this aspect is concerned, the literature advocates between 30 seconds and 3 minutes of ultrasonic activation of the irrigant [36], but there is still no consensus concerning application time [37,36]. In the present study, the decision was taken to use the ultrasound for 60 seconds and it was found that, regardless of irrigation solution and root third, PUI of the irrigant did not interfere with the bond strength of the glass-fiber post. This result may be attributable to ultrasound’s inefficiency in improving removal of the smear layer and providing the opening of the dentinal tubules [35,26]. However, other researchers have reported that PUI had a favorable effect on the removal of smear layer during endodontic treatment [38,27,39], in this study, the explanation for the fact that PUI did not have a significant effect can be due to the fact that, although the elliptic-shaped teeth were replaced by others with more circular conformation, the fiber post did not present juxtaposed in all the roots. As a result, there was a greater thickness of resin cement and, consequently, a possible benefit generated by the use of ultrasonic activated irrigants became statistically insignificant due to the inherent variability of the resistance values.

Given that ultrasonic vibration leads to the agitation of the irrigation solution in all directions, it is important to evaluate if there is any risk of apical infiltration and consequent damage to periodontal tissue and alveolar bone. In the present study, there was no extrusion of the irrigant due to the root canal models having had a solid foramen, sealed with composite resin. [37], however, reported that the risk of irrigation solution overflowing into the periapical region is reduced when PUI is used, due to the direction of oscillation of the tip being lateral and not longitudinal.

In the present study, there was no significant difference between bond strength values obtained from the cervical, middle and apical thirds. This discovery corroborates the findings of other studies in that there was a statistically significant difference compared to the irrigation solution, though not between the root thirds [40,29].

With regard to fracture analysis, it should be pointed out that the predominant type of failure was the adhesive between the dentin and the cement when using the irrigant EDTA at 17%, regardless of the canal region (cervical, middle or apical) and of the use, or not, of PUI which, clinically, would be expressed in the decementation of the post. However, bearing in mind that the bond strength values for the group irrigated using EDTA exceeded those found with the use of chlorhexidine and saline solution, up to the point of decementation, a greater force would be required for this event to occur. Mixed failures were more prevalent when using the irrigants 2% chlorhexidine digluconate and 2.5% sodium hypochlorite, a result which was also observed in the group treated with saline solution. Failures of the post-cement adhesive type had lower indices, regardless of whether PUI was performed or not, or of the root third, this finding probably being due to the fact that silane was used. Cohesive fractures in dentin were also less frequent, which may be explained by the fact that fragility of the bond occurs at the interfaces [29].

Based on the results of this study, it was concluded that the bond strength of the glass-fiber post at the different depths of root dentin was influenced by the irrigating agent, regardless of whether or not PUI was used. It is noteworthy that there is evidence that the association of EDTA and NaOCl provides optimized endodontic results with respect to the bond strength of fiber posts to the root canal [29]. In this sense, it would be interesting to evaluate the effect of these associated agents, considering the use of PUI. As well as the need for further investigations, regarding in terms of the length of time the passive ultrasonic irrigation in used and the longevity of the union of fiber posts when the PUI is used.

**5. Conclusion**

The bond strength of the glass-fiber post to radicular dentin, whether cervical, middle or apical, was influenced by the irrigating agent, the best results being obtained using EDTA at 17%, when compared with 2% chlorhexidine digluconate and saline solution, regardless of the PUI.

**Acknowledgement**

This research did not receive any specific grant from funding agencies in the public, commercial, or not-for-profit sectors.

References

[1] Ferrari M, Vichi A, Grandini S, Goracci C. Efficacy of a self-curing adhesive-resin cement system on luting glass-fiber posts into root canals: an SEM investigation. [International Journal Prosthodont.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Efficacy+of+a+self-curing+adhesive-resin+cement+system+on+luting+glass-fiber+posts+into+root+canals%3A+an+SEM+investigation)2001Nov-Dec;**14**(6):543-9.

[2] Prado M, Simão RA, Gomes BP. Effect of different irrigation protocols on resin sealer bond strength to dentin. Journal Endodontics. 2013 May;**39**(5):689-92.

[3] Agrawal VS, Kapoor S. An in vitro scanning electron microscopic study comparing the efficacy of passive ultrasonic and syringe irrigation methods using sodium hypochlorite in removal of debris from the root canal system. Journal - Irish Dental Association. 2012 June-July;**58**(3):156-61.

[4] Aranda-Garcia AJ, Kuga MC, Vitorino KR, Chavez-Andrade GM, Duarte MAH, Bonetti-Filho I et al. Effect of the root canal ﬁnal rinse protocols on the debris and smear layer removal and on the push-out strength of an epoxy-based sealer. [Microscpy Research Techinique.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Effect+of+the+root+canal+%EF%AC%81nal+rinse+protocols+on+the+debris+and+smear+layer+removal+and+on+the+push-out+strength+of+an+epoxy-based+sealer) 2013 May;**76**(5):533-7.

[5] Haapasalo M, Shen Y, Qian W, Gao Y. Irrigation in endodontics. Dental Clinics of North America. 2010 Apr;**54**(2):291-312.

[6] Só MVR, Vier-Polisser FV, Darcie MS, Smanioto DGR, Montagner F, Kuga MC. Dissolução do tecido pulpar quando do uso do hipoclorito de sódio e EDTA isoladamente ou associados. Revista Odonto Ciência. 2011;**26**(2):156-60.

[7] Magro MG, Kuga MC, Victorino KR, Vazquez-Garcia FA, Aranda-Garcia AJ, Faria Júnior NB et al. Evaluation of the interaction between sodium hypochlorite and several formulations containing chlorhexidine and its effect on the radicular dentin – SEM and push-out bond strength analysis. [Microscopy Research Technique.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Evaluation+of+the+interaction+between+sodium+hypochlorite+and+several+formulations+containing+chlorhexidine+and+its+effect+on+the+radicular+dentin+%E2%80%93+SEM+and+push-out+bond+strength+analysis) 2014 Jan;**77**(1):17-22.

[8] Dornelles-Morgental R, Guerreiro-Tanomaru JM, de Faria-Junior NB, Hungaro-Duarte MA, Kuga MC, Tanomaru-Filho M. Antibacterial efficacy of endodontic irrigating solutions and their combinations in root canals contaminated with *Enterococcus faecalis*. [Oral Surgery Oral Medicine Oral Pathology Oral Radiology Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Antibacterial+efficacy+of+endodontic+irrigating+solutions+and+their+combinations+in+root+canals+contaminated+with+Enterococcus+faecalis) 2011 Sept;**11**2(3):396-400.

[9] Prado M, Simão RA, Gomes BP. Evaluation of different irrigation protocols concerning the formation of chemical smear layer. Microscopy Research Technique. 2013 Feb;**76**(2):196-200.

[10] Saif S, Carey CM, Tordik PA, McClanahan SB. Effect of irrigants and cementum injury on diffusion of hydroxyl ions through the dentinal tubules. Journal of Endodontics. 2008 Jan;**34**(1):50-2.

[11] Moreira DM, Almeida JFA, Ferraz CCR, Gomes BPFA, Line SRP, Zaia AA. Structural analyses of bovine root dentin after use of different endodontics auxiliary chemical substances. [Journal of Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/19567327) 2009 July;**35**(7):1023-7.

[12] Kishen A, Sum CP, Mathew S, Lim CT. Influence of irrigation regimens on the adherence of Enterococcus faecalis to root canal dentin. [Journal of Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Influence+of+irrigation+regimens+on+the+adherence+of+Enterococcus+faecalis+to+root+canal+dentin) 2008 July;**34**(7):850-4.

[13] Hong ST, Bae KS, Baek SH, [Kum KY](http://www.ncbi.nlm.nih.gov/pubmed/?term=Kum%20KY%5BAuthor%5D&cauthor=true&cauthor_uid=21092820), [Shon WJ](http://www.ncbi.nlm.nih.gov/pubmed/?term=Shon%20WJ%5BAuthor%5D&cauthor=true&cauthor_uid=21092820), [Lee W](http://www.ncbi.nlm.nih.gov/pubmed/?term=Lee%20W%5BAuthor%5D&cauthor=true&cauthor_uid=21092820). Effects of root canal irrigants on the push-out strength and hydration behavior of accelerated mineral trioxide aggregate in its early setting phase. [Journal of Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Effects+of+root+canal+irrigants+on+the+push-out+strength+and+hydration+behavior+of+accelerated+mineral+trioxide+aggregate+in+its+early+setting+phase) 2010 Dec;**36**(12):1995-9.

[14] Bitter K, Hambarayan A, Neumann K, Blunck U, Sterzenbach G. Various irrigation protocols for final rinse to improve bond strengths of fiber posts inside the root canal. [European Journal of Oral Sciences.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Various+irrigation+protocols+for+final+rinse+to+improve+bond+strengths+of+fiber+posts+inside+the+root+canal) 2013 Aug;**121**(4):349-54.

[15] Ekambaram M, Yiu CKY, Matinlinna JP, Chang JW, Tay FR, King NM. Effect of chlorhexidine and ethanol-wet bonding with a hydrophobic adhesive to intraradicular dentine. [Journal Dentistry.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Effect+of+chlorhexidine+and+ethanol-wet+bonding+with+a+hydrophobic+adhesive+to+intraradicular+dentine) 2014 July;**42**(7):872-82.

[16] Jiang LM, Verhaagen B, Versluis M, Langedijk J, Wesselink P, van der Sluis LWM. The influence of the ultrassonic intensity on the cleaning efficacy of passive ultrasonic irrigation. [Journal of Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/?term=The+influence+of+the+ultrassonic+intensity+on+the+cleaning+efficacy+of+passive+ultrasonic+irrigation) 2011 May;**37**(5):688-92.

[17] Mozo S, Llena C, Forner L. Review of ultrassonic irrigation in endodontics: increasing action of irrigating solutions. [Medicine Oral Patology Oral Cir Bucal.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Review+of+ultrassonic+irrigation+in+endodontics%3A+increasing+action+of+irrigating+solutions.) 2012 May 1;**17**(3):e512-6.

[18] Vinhorte MC, Suzuki ES, Carvalho MS, Marques AAF, Sponchiado Jr EC, Garcia LFR. Effect of passive ultrasonic agitation during final irrigation on cleaning capacity of hybrid instrumentation. [Restorative Dental Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Effect+of+passive+ultrasonic+agitation+during+final+irrigation+on+cleaning+capacity+of+hybrid+instrumentation) 2014 May;**39**(2):104-8.

[19] Bueno CES, Pelegrine RAP,  Silveira CFMS, Bueno VCPS, Alves VO, Cunha RS et al.The impact of endodontic irrigating solutions on the push-out shear bond strength of glass fiber posts luted with resin cements. [General Dentistry.](http://www.ncbi.nlm.nih.gov/pubmed/?term=The+impact+of+endodontic+irrigating+solutions+on+the+push-out+shear+bond+strength+of+glass+fiber+posts+luted+with+resin+cements) 2016 Jan-Feb;**64**(1):26-30.

[20] Vangala A, Hegde V, Sathe S, Dixit M, Jain P. Effect of irrigating solutions used for postspace treatment on the push-out bond strength of glass fiber posts. [Journal of Conservative Dentistry.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Effect+of+irrigating+solutions+used+for+postspace+treatment+on+the+push-out+bond+strength+of+glass+fiber+posts) 2016 Jan-Feb;**19**(1):82-6.

[21] Serafino C, Gallina G, Cumbo E, Monticelli F, Goracci C, Ferrari M. Ultrasound effects after post space preparation: an SEM study. Journal of Endodontics. 2006;**32**:549-52.

[22] Desai P, Himel V. Comparative safety of various intracanal irrigation systems. Journal of Endodontics. 2009 Apr;**35**(4):545-9.

[23] Xin-Hua Gu, Cai-Yun Mao and Matthias Kern. Effect of Different Irrigation on Smear Layer Removal after Post Space Preparation. Journal of Endodntics. 2009; **35**(4): 583-586

[24] Uroz-Torres D, González-Rodríguez MP, Ferrer-Luque CM. Effectiveness of the EndoActivator System in removing the smear layer after root canal instrumentation. [Journal of Endod.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Effectiveness+of+the+EndoActivator+System+in+removing+the+smear+layer+after+root+canal+instrumentation) 2010 Feb;**36**(2):308-11.

[25] Pucci CR, Carvalho CAT, Vasconcelos RA, Lacerda AJF, Gullo M, Xavier ACC, Gonçalves SEP, Rêgo HMC. Effect of laser, ultrasound and irrigation solutions on bond-strenght of fiberglass-posts. Dental Journal Materials. 2103 Sept; **29**(1): 176-186.

[26] Martinho FC, Carvalho CAT, Oliveira LD, Lacerda AJF, Xavier ACC, Augusto MG, Zanatta RF, Pucci CR.Comparison of different dentin pretreatment protocols on the bond strength of glass fiber post using self-etching adhesive. [Journal of Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Effect+of+cement+type%2C+relining+procedure%2C+and+length+of+cementation+on+pull-out+Bond+strength+of+fiber+posts) 2015 January;**41**(1):83-7.

[27] Lui JN, Kuah HG, Chen NN. Effect of EDTA with and without surfactants or ultrasonics on removal of smear layer. [Journal of Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/17368342) 2007 Apr;**33**(4):472-5. Epub 2007 Feb 20.

[28] Goel S, Tewary S. Smear layer removal with passive ultrasonic irrigation and the NaviTip FX: a scanning electron microscopic study. Oral Surgery Oral Medicine Oral Pathology Oral Radiology Endodontics. 2009 Sept;**108**(3):465-70.

[29] Kul E, Yeter KY, Aladag LI, Ayrancı LB. Effect of different post space irrigation procedures on the bond strength of a fiber post attached with a self-adhesive resin cement. Journal of Prosthetic Dentistry. 2016 May;**115**(5):601-5.

[30] Bitter K, Paris S, Pfuertner C, Neumann K, Kielbassa AM. Morphological and bond strength evaluation of different resin cements to root dentin. European Journal Oral Science. 2009 June;**117**(3):326-33..

[31] Ari H, Yasar E, Belli S. Effects of NaOCl on bond strengths of resin cements to root canal dentin. Journal of Endodontics. 2003;**29**:248-51.

[32] Di Hipólito V, Rodrigues FP, Piveta FB, Azevedo LC, Alonso RCB, Silikas N, Carvalho RM, De Goes MFuarte MAH, D`Alpino PHP. Effectveness of self-adhesive luting cements in bonding to chlorhexidine-treated dentin. Dental Materials 2012;**28**:495-501.

[33] Araújo DFG, Chaves LP, Bim Júnior O, Garcia FCP, Ishikiriama SK, Honório HM et al. Influence of 2% chlorhexidine digluconate on bond strength of a glass-fibre post luted with resin or glass-ionomer based cement. [Journal Dentistry.](http://www.ncbi.nlm.nih.gov/pubmed/24613604) 2014 June;**42**(6):735-41.

[34] Ekambaram M, Yiu CKY, Matinlinna JP, Chang JW, Tay FR, King NM. Effect of chlorhexidine and ethanol-wet bonding with a hydrophobic adhesive to intraradicular dentine. [Jurnal Dentistry.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Effect+of+chlorhexidine+and+ethanol-wet+bonding+with+a+hydrophobic+adhesive+to+intraradicular+dentine) 2014 July;**42**(7):872-82.

[35] Gu LS, Kim JR, Ling J, Choi KK, Pashley DH, Tay FR. Review of contemporary irrigant agitation techniques and devices. [Journal of Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Review+of+contemporary+irrigant+agitation+techniques+and+devices) 2009June;**35**(6):791-804.

[36] Munley PJ, Goodell GG. Comparisson of passive ultrasonic debridement between fluted and nonfluted instruments in root canals. [Journal of Endodontics.](http://www.ncbi.nlm.nih.gov/pubmed/?term=Comparisson+of+passive+ultrasonic+debridement+between+fluted+and+nonfluted+instruments+in+root+canals) 2007 May;**33**(5):578-80. Epub 2007 Mar 13.

[37] Tasdemir T, Er K, Celik D, Yildirim T. Effect of passive ultrasonic irrigation on apical extrusion of irrigating solution. European Journal Dentistry. 2008 July;**2**(3):198-203

[38] Gutarts R, Nusstein J, Reader A, et al. In vivo debridement efficacy of ultrasonic irri- gation following hand-rotary instrumentation in human mandibular molars. Journal of Endodontics 2005;**31**:166-70.

[39] van der Sluis LW, Versluis M, Wu MK, Wesselink PR. Passive ultrasonic irrigation of the root canal: a rewiew of the literature. International Endodontic Journal. 2007 June;**40**(6):415-26. Epub 2007 Apr 17.

[40] Silveira OC, Silva RB, Dametto FR, Machado CT, Santos AJS, Cavalcante AL. Effect of endodontic irrigating solutions on the micro push-out bond strength of a fibre glass dowel. Acta stomatologica Croatica. 2014;**48**(1):16-24.